Specification of Cylindrical Lithium ion

Battery

Type: ICR26650

TEL: 0086 755 36936900

FAX: 0086 755 36936933

E-mail:sales@battery-matrix.com

Http://www.battery-matrix.com

Factory: Building B, 3RD Industrial Zone,

Shenkeng Village, Henggang Town, Shenzhen

| Edited by | Checked by | Authorized by |
| --- | --- | --- |
| Lin lin | Baike | Hangbin dou |

### Index of specification

Type -------------Air proof cylindrical rechargeable Li-ion battery

Model ------------------------------------------------------------- ICR26650

H

D

Size type--------------------------------------------------------------- 26650

Nominal voltage------------------------------------------------------ 3.7V

Weight --------------------------------------------------------Approx. 90g

C5mAh------------------------------------------------------------- 4000mAh

Charging Voltage------------------------------------------ 4.200±0.049V

Min. discharging cut-off Voltage-------------------------------- 2.75V

Max. Charging cut-off Voltage ---------------------------------- 4.20V

Max. Continuous charging current--------------------------- 8000mA

Max. Continuous discharging current ---------------------- 12000mA

Size (Including shrinkage tube)

Diameter ------------------------------------------------------ 26.2±0.1mm

Height---------------------------------------------------------- 64.7±0.3mm

Capacity (20oC, 0.2 C5 to 2.75V)

Minimum capacity---------------------------------------------4080mAh

Impedance（ 20℃5℃, fully charged）------------------- ≤80mΩ

Charging Term (20oC):

Standard charging------ First at 2000mA of current charged to 4.2V;

then by constant current to the minimum drain of 20mA

Speedy charging---- 2000mAto 4.2V, then constant voltage to 20mA

Working Ambient（Suggested）

Stock-----------------------------------------------------------Temp. (15-35℃)

--------------------------------------------Relative humidity (45-75%)

-----------------------------------------------Air pressure (86-106Kpa)

Discharging------------------------------------------------------------ -20-60℃

Standard charging------------------------------------------------------- 0-45℃

Relative humidity -------------------------------------------------------- <93%

Air pressure---------------------------------------------------------- 86-106kPa

Standard Testing Ambient (Except special requirements)

Temperature---------------------------------------------------------- 20℃±5℃

Relative humidity----------------------------------------------------- 65±20%

Remark: All the details subjected to the new version, in case if there is any amendment, forgive us not other notice.

1. General Performance

| Testing items | Testing Condition | Approval requirements |
| --- | --- | --- |
| - Outside appearance | Naked eye sight checking | No rupture & distortion, No besmirch & leakage |
| (2) Standard Testing Condition | Except special requirement, should be under the condition of: Temp. of 20±5℃, Humidity of 65±20% |  |
| (3) Standard Charging | Referring under the20+5℃，65±5%RH，1）Charged at 0.5It mA to 4.2V(every single battery)，2）Turn to charging at a constant voltage of 2V until the current least 20mA，then stop here. |  |
| (4) Speedy Charging | Referring to under the condition of 20+5℃，65±5%RH，1）Charged at 1It mA constant current to 4.2V(every single battery)，2）At constant voltage of 4.2V charging until the current less 20mA, cut off. |  |
| (5)Shipping V. | Checked before delivery | ≥3.75V |
| (6)Nominal Capacity | Referring to at the condition of 20+5℃，65±5%RH，1）Before charging, discharging at 0.2It mA at constant current to 2.75V cut off；2）then rest 10 minutes；3） discharging at 0.2ItmA to 2.75V, this is the capacity | Discharging capacity: ≥100%C5mAh |
| （7）speedy Discharging Capacity | Under the condition of 20+5℃，65±5%RH，1）First discharge at 0.2It mA constant current to 2.75V cut off；2）Resting 10 minutes after a standard charging；3）Discharging at 1It mA to 2.75Vcut off, this is the speedy discharging capacity | Discharging capacity: ≥90%C5mAh |
| (8) Cycle Life | 1) Resting 10 minutes after standard discharging, 2)At condition of 20+5℃，65±5%RH，charged at 4000mA to full, then resting 10 minutes，3)Discharged at 4000 mA to the cut off voltage 2.75V, 4)Repeat 2) and 3) cycles，stop until its capacity less than 80%C5mAh. | ≥600 cycles |
| (9) -20℃ Discharging Characteristic | 1)A standard charged first；2) At the temp. of -20℃2℃layig aside 16h～24h；3)Discharging at 0.2It mA constantly to the cut off 2.75V under the temp of-20℃2℃；4）Calculate its capacity | Discharging capacity: ≥60%C5mAh |

2 Mechanism traits

| Testing items | Testing condition | Approval requirements |
| --- | --- | --- |
| (1) Vibration Test | At ordinary temp. put the fully charged cell on the platform of vibration lasting 30 minutes as per the following: Displacement：0.38mm(10-30Hz)；0.19mm（30-55Hz） Frequency：10-55Hz(1oct/min) Directions：X,Y | No leakage, blast, fire, no defective of performance and appearance |
| (2)Drop Impact | Let the fully charged cell fall to the board of 5cm thickness horizontally placed at the height of 1m. | No leakage, blast, fire, no defectiveof performance and appearance |

3 Safe characteristic

| Testing Items | Testing Condition | Approval requirements |
| --- | --- | --- |
| (1) Oven Test | Put the fully charged cells into the heating oven at a rate of 5±2℃/minute up to 150±2℃, and then bearing there 30 min. | No fire, No explode. |
| (2)Shot Cut Test | By a wire bearing 26A (impedance≤26mΩ) connecting the positive and negative of a cell fully charged, stop while the cell temp. down 10℃ comparing the peak temp. | No fire, No explode. |
| (3)Over charged test | Discharged at 1ItmA cut off at 2.75V, and then charging at 3ItmA 4.6V; charging 8 hours. | No fire, No explode. |
| (4)Soaking Test | Soaking the fully charged cells to the water of ambient temperature lasting 24 hours | No fire, No explode. |

4 Protective characteristics

When the li-ion works at the voltage above the permitted (or current), the electrolyte could be decomposed; it will damage its safety. While the voltage below 1.0V, its performance will be a kind of depravities. Therefore, calls must be protected by heating fuse and PCM to avoid over charging, over discharging, over current.  The fuse connecting with the PCM, and make it possible closer to stick the shell of the battery.

Recommend the PCM as the following parameter (Single PCM):

Over charging test Voltage           ：     4.250±0.025V

Over charging releasing Voltage      ：     4.175±0.050V

Over discharging test Voltage        ：     2.30±0.08V

Over discharging releasing Voltage   ：     2.40±0.10V

Over current testing                 ：     ≤8A（only for reference）

5 Warranty

Within 6 months after aparting from our factory.

6 Using guide

Do not heat or dispose into the fire.

Do not try to connect the positive and negative with a wire.

Do not disassemble the battery.

Do not weld the battery directly.

Using and stocking the battery away from the ambient of static.

Do not mix other brand battery (different spec.) for the using, packing.

In case the electrolyte spillage on your skin, wash it with clear water immediately.

If into your eyes, you need to go further to see a doctor at once after washing.

Keep the battery out of reach of children and infant prevent swallowing.

The functional temperature range;

Charging   ：0℃~45℃

Discharging：-20℃~60℃